## Slide 1: A Spherical Cow Approximation to Symmetric Li Ion Cells
Javier Bareño

## Slide 2: Spherical Cow Approximation
Cell behavior is approximated by the V-Q characteristic of each electrode, interpolated from experimental results in half cells
Different mechanisms shift and/or alter the Li inventory and electrode loading
Cell V is calculated as the V difference between electrodes
Kinetic effects are not considered, other than (possibly) introducing an ad-hoc overpotential to approximate internal resistance and polarization
Keenan Crane
http://www.cs.cmu.edu/~kmcrane/Projects/ModelRepository/

## Slide 3: Ideal Symmetric Cell
We start from a cell consisting of two NCM523 electrodes, each charged to 4.0 V v. Li/Li+
Each NCM523 electrode is approx. 54% full of Li
Cell voltage is 4.0 V – 4.0 V = 0 V

## Slide 4: Ideal Symmetric Cell: 1st Charge
As the cell charges to 0.5 V, Li moves from cathode to anode
Cell is balanced, each electrode changes SOC by same amount
No internal red/ox currents: measured cell capacity matches electrode EOS change

## Slide 5: Ideal Symmetric Cell: 1st Discharge
Upon cell discharge to 0 V, Li goes back to the cathode
No Li inventory change or shift:
  Discharge capacity matches charge capacity
  Both electrodes go back to initial 4.0 V v. Li

## Slide 6: Ideal Symmetric Cell: Cycling
Upon cycling:
  Charge keeps constant
  No V drift

## Slide 7: Active Material Loss
A process that effectively reduces the loading of one or both electrodes
E.g. , particle disconnection from current collector
May result in loss of Li inventory, depending on SOC of lost material
Does not change the effective SOC of the remaining material and does not require a compensating current

## Slide 8: AML: Cathode Loss at Top of Charge First Charge
Initial charge to 0.5 V similar to ideal cell case

## Slide 9: AML: Cathode Loss at Top of Charge Loss of AM at cathode
At top of charge, 65% of cathode active material is lost; e.g., particle disconnection during a hold
The loss does not change the SOC of any electrode, but reduces the capacity (Li intercalation sites) of the cathode

## Slide 10: AML: Cathode Loss at Top of Charge First Discharge
During discharge, Li travels back from anode to cathode
It takes (65%) less Li to discharge the cathode back to 4.0 V v Li than it took to charge it before AM loss
There is still Li at the anode

## Slide 11: AML: Cathode Loss at Top of Charge First Discharge
The cell continues to discharge, and VC continues to drop, until both electrodes reach same potential (lower than discharged state before cathode loss)
Less Li comes back from the anode than what was charged: Q_disch < Q_ch

## Slide 12: AML: Cathode Loss at Top of Charge Second Charge
In the discharged cell, both electrodes sit at lower potential v. Li
During the second charge, it takes the same amount of Li as in first discharge to return each electrode to the same charged SOC

## Slide 13: AML: Cathode Loss at Top of Charge Extended cycling
5% cathode AM loss at top of each charge
Electrode voltages at top of charge remain constant
Electrode voltages at bottom of discharge keep falling
Cell capacity drops
QD = QCprevious

## Slide 14: AML: Cathode Loss at Bottom of Discharge Extended cycling
5% cathode AM loss at bottom of each discharge
Does not change electrode voltages, which remain constant at bottom of discharge
Li loss from lithiated cathode loss:
  100% CE
  Cell capacity drops
  Electrode V at top of charge increases

## Slide 15: AML: Anode Loss at Top of Charge Extended cycling
5% anode AM loss at top of each charge
Does not change electrode SOC, VA/C in charged cell constant
Li loss from lithiated anode drives electrode V increase in discharged cell

## Slide 16: AML: Anode Loss at Bottom of Discharge Extended cycling
5% anode AM loss at bottom of each discharge
Does not change electrode SOC, VA/C in discharged cell constant
VA/C drops in charged cell because anode cannot accept all Li from cathode upon charge

## Slide 17: AML: Extended Cycling Comparison
Voltage creep occurs at opposite end of charge-discharge cycle to active material loss
Direction of voltage creep switches with anode or cathode loss and with end of C-D cycle at which AML occurs

## Slide 18: AML: Extended Cycling Comparison
First half cycle is charge
CE = QD/Qcprevious
CR = QC/Qdprevious
AML leads to Qcell loss in all cases
AML at top of charge: coulombic inefficiency
AML at bottom of discharge: capacity loss between cycles

## Slide 19: Next Steps
Explore the effect of redox currents:
  Li inventory change and/or shift
  Mismatch between measured Qcell and electrode SOC changes
  No associated AML
Explore the effect of Li reorganization
  Redox effects without compensating current
  Causes AML
Compare to experimental data (KK48RT3)

## Slide 20: Li reorganization / phase transitions
After initial charge to 0.5 V, 25% of cathode is lost but its Li is transferred to the remaining cathode
This causes cathode self discharge, with no Qcell nor changing anode SOC

## Slide 21: Li reorganization / phase transitions
During a voltage hold, external Qcell needs to be supplied to recharge the cell after the cathode self discharge
Can be approximated by a series of charge-phase transition cycles